## Slide 1: 2024 HEPCAT report: kinetic inductance phonon-mediated detectors
Zoë Smith
Me!

## Slide 2: Why we need phonon mediated detectors
O.Wen Journal of Low Temperature Physics (2022) 209:510–517
Sub-GeV dark matter candidates require sub keV energy resolution.
In Si target, 100 MeV dark matter would deposit ~1eV.
Resolutions of ~3 eV have been shown in TES based detectors.
Phonon absorption and quasiparticle poisoning also important question in QIS community

## Slide 3: Outline
Device Principle
KIPM Fabrication @ Stanford
Low Tc KIPM development
Trapped flux problem
Phonon collection measurements
MEMs mirror setup for KIPMs

## Slide 4: MKIDs utilize Kinetic Inductance.
KI comes from charge carriers resisting change in motion in a changing electric field
KI changes with the number of charge carriers!
L
C

## Slide 5: MKIDs as phonon Detectors
Some dark matter candidates can create phonons in crystal substrate
Phonons that are absorbed into superconducting Al can break cooper pairs
Broken cooper pairs change KI, and therefore resonant frequency and dissipation of MKID

## Slide 6: Designing KIDs for Dark matter = KIPMs
Phonon collection efficiency… need this to be high!
Ways to tune KIPMs for large signal to noise:

## Slide 7: KIPM fabrication at Stanford
1. RCA Clean Si Wafer
2. RF clean and sputter Al, AlMn or Hf
5. Etch metal:
Al/AlMn- wet etch in Al Etchant
Hf- wet etch in HF
Nb- Dry etch
3. Expose Pattern
4. Develop PR
Repeat steps 2-5 if including Nb wiring.

## Slide 8: Low-Tc KID development
Making and testing Low Tc MKIDs
Resolution increases by decreasing superconducting gap
Hafnium device fabbed by Miguel Daal from UCB
Aluminum device fabbed by Osmond Wen at Caltech
AlMn by me, working on getting Hf at Slac
Hf
Tc: ~400mK
Al
Tc: 1.2K
AlMn
Tc: 630 mK

## Slide 9: Losses from trapped vortices
struggled to get consistent quality factors
Believe trapped vortices in the superconducting films contributes to this
Adding flux traps can mitigate this

## Slide 10
I. Nsanzineza and B. Plourde, Phys. Rev. Lett. 113, 117002 (2014)
Field cooling measurements & fab by K. Okubo @ Syracuse

## Slide 11: KIPM phonon setup
Installed RF readout and optical fiber chains into our cryostat
We pulse an LED on the back of KIPM while cold and measure changes in RF transmission.

## Slide 12: Phonon resolution measurements
Implementing phonon collection efficiency measurement
this has become a standard technique we use for KIDs, based on success with TES-based detectors
Fitting mean vs variance allows for establishing an absolute energy scale due to photon variance
In progress…

## Slide 13: Phonon collection efficiency problem
Collaborators at Caltech & Fermilab have shown ~2eV baseline resolution, but <1% phonon collection efficiency using the shot noise measurement
Many possible losses to balance
Si
Detector
High gap superconductor
Gold or copper mounts
Gold or copper mounts
Rough edges
Sources of phonon loss

## Slide 14: Next up: changing where LED hits chip
Fermilab designed a prototype MEMs system to steer beam.
SLAC group resigned to fit inside 5” cryoperm can
Enables testing in a light-tight & low magnetic field environment
lid for Magnetic Shield
K. Stifter arXiv:2405.02258)
Notes: reflective collimation and fixed positions of mirrors based on v1 design

## Slide 15: Thanks to the support of HEPCAT I have…
gained valuable instrumentation experience installing RF and optical systems into cryostats
designed multiple fabrication recipes for superconducting detectors
helped maintain vacuum and cryogenic systems for fabrication
applied shot noise measurements for KIPMs

## Slide 16: Thank you!
DMQIS group…
Noah Kurinsky (Scientist)
Kelly Stifter (Scientist)
Betty Young (SC Faculty)
Nico Linton (Technician)
Sidney Stevens (Mech. Eng.)
Jamie Ryan (Postdoc)
Chiara Salemi (Porat Fellow)
Taylor Aralis (Postdoc)
Jadyn Anczarski (Stanford grad)
Taj Dyson (Stanford grad)
Aviv Simchony (Stanford grad)
Zoe Smith (Stanford grad)
Hannah Magoon (Stanford grad)
Tonya Peschel (SLAC post-bac)
Giana Perez (Stanford ugrad)
Anthony Nunez (Stanford ugrad)
Elizabeth Panner (Tufts ugrad)
Charles Snipp (Stanford ugrad)

## Slide 17: MKIDs are LC circuits.
L
C
LC circuits are harmonic oscillators
Their resonance frequency is:

## Slide 18: MKIDs operate at Microwave Frequencies.
shelf electronics in microwave regime
MuWe design our LC circuits to be in 4-8 GHz regime for various reasons:
  KI better when charges travel shorter distance
    Keep resonance frequency much lower than gap frequency
  Off the ltiplexing!
Shawn W. Henderson, 2018

## Slide 19: We couple the MKID to a transmission line.
Send microwave with known phase and amplitude down feedline
Couple a device (MKID!) to feedline & distort microwave:
Qr total quality factor (Qi+Qc)/(QiQc)
Qc depends on coupling to feedline
  is fixed for given design
Qi relates to dissipation of energy in the film
1
(in)
2
(out)
DUT

## Slide 20: Backup: Pulses!
Samples
df/f

## Slide 21: Multiplexing and Quality factors:
How dense can you pack them?
FWHM
Frequency
|S21|
fr

## Slide 22: MKIDs utilize Kinetic Inductance.
KI comes from charge carriers resisting change in motion in a changing electric field
KI changes with the number of charge carriers!
Geometric Inductance… does not
Want to increase KI fraction (within reason):
L
C

## Slide 23: Backup: Magnetic Shields!